## Slide 1: Enhancing Safety of Hydrogen Containment Components Through Materials Testing Under In-Service Conditions
B.P. Somerday, J.A. Campbell, K.L. Lee, J.A. Ronevich, and C. San Marchi
Sandia National Laboratories, Livermore CA, USA
6th International Conference on Hydrogen Safety (ICHS 2015)
Yokohama, Japan
October 21, 2015
Sandia is a multiprogram laboratory operated by Sandia Corporation, a Lockheed Martin Company, for the United States Department of Energy under contract DE-AC04-94AL85000

## Slide 2: Hydrogen can permeate into containment materials and activate hydrogen embrittlement
Mobility of H at ambient temperature distinguishes it from other embrittlement species (e.g. S, P)
sremote
slocal, elocal
sremote
slocal, elocal
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
H2
hydrides
H
H
H
H
H
H
H
H
HEDE
H
t1
t2
H
H
H
H
H
H
H
H
H
H
H
H
H
H
t1 > t2
HELP

## Slide 3: Materials in range of H2 containment components can be susceptible to hydrogen embrittlement
stationary and transport vessels
(martensitic steels)
pipelines
(ferritic steels)
on-board tanks
(stainless steel boss)
manifold components
(stainless steels)

## Slide 4: Hydrogen embrittlement accelerates crack extension, potentially compromising component safety
Hydrogen embrittlement accounted for in design and safety qualification through materials testing
Barthélémy, 1st ESSHS, 2006
a
Number of pressure cycles, N
crack in H2
crack in N2
H2
H2
H2
H2
Dp
a
H2
H2
H2
H2

## Slide 5: Dynamic-Load Testing in High-Pressure H2 Gas: concurrent mechanical loading and H2 exposure
Dynamic mechanical loading
  Monotonic or cyclic
Operating envelope
  H2 gas pressure up to 138 MPa
  Load-cycle frequency from 10-3 to 10 Hz
  Room temperature
Instrumentation
  Internal load cell
  LVDT-based displacement gauges
  Direct-current potential difference crack measurement system

## Slide 6: Static-Load Crack Growth Testing in H2 Gas: concurrent mechanical loading and H2 exposure
Static mechanical loading
  Constant displacement imposed by bolt reacting against pin
Operating envelope
  H2 gas pressure up to 200 MPa
  Temperature chamber: -70 to 170 oC
Instrumentation
  Reaction pins with strain gauges serve as load cells
time
load
KTHa
crack extension
da/dt

## Slide 7: Thermal Precharging in H2 Gas: mechanical loading follows H2 exposure
Operating envelope
  H2 gas pressure up to 138 MPa
  Furnace temperature up to 300 oC
Dynamic or static mechanical loading
  Subsequent to H2 gas exposure
Instrumentation
  Load cells and displacement gauges on mechanical test frames

## Slide 8: Steel pressure vessels store high-pressure compressed hydrogen at refueling stations
ASME developed Article KD-10 in Section VIII-3 of Boiler and Pressure Vessel code for high-pressure H2 vessel design
  “Special Requirements for Vessels in High Pressure Gaseous Hydrogen Service”
  Mandatory for seamless vessels with H2 pressure > 41 MPa and welded vessels with H2 pressure > 17 MPa (upper limit 100 MPa)
KD-10 requires fracture mechanics measurements on containment materials in high-pressure H2 gas

## Slide 9: Design life analysis in ASME Article KD-10 requires data from materials testing in H2 gas
H2
H2
H2
H2
Dp
ao
H2
H2
H2
H2
Materials testing must be performed in the service environment: high-pressure H2 gas

## Slide 10: Fatigue crack growth relationships measured for Cr-Mo pressure vessel steel in high-pressure H2 gas
Materials
  Three different heats of SA-372 Grade J
Instrumentation
  Internal load cell in feedback loop
  Crack-opening displacement measured internally using LVDT
  Crack length calculated from compliance
Mechanical loading
  Triangular load-cycle waveform
  Constant load amplitude
  Load-cycle frequency = 0.1 Hz
Environment
  99.9999% H2 supply gas
  Pressure = 100 MPa
  Room temperature

## Slide 11: Measurements reveal significant effect of H2 gas on fatigue crack growth rates for SA-372 Gr. J steel
Accelerated crack growth rates in H2 gas can be accounted for in pressure vessel design through analysis
B. Somerday, C. San Marchi, K. Nibur, ASME PVP, 2013

## Slide 12: Design life analysis in ASME Article KD-10 accounts for effect of H2 gas on fatigue crack growth rates
Analysis determines number of pressure cycles for safe operation of pressure vessel
da/dN=CDKm
DK = Dp[f(a, t ,Ro, Ri)]

## Slide 13: Summary
Hydrogen embrittlement accounted for in design and safety qualification of components through materials testing
Sandia National Laboratories features three systems for materials testing in H2 gas:
  Dynamic-Load Testing in High-Pressure H2 Gas
  Static-Load Crack Growth Testing in H2 Gas
  Thermal Precharging in H2 Gas
  Distinguishing feature: high-pressure (>138 MPa) H2 gas
Materials testing at Sandia National Laboratories motivated by developing and exercising standards
  Fatigue crack growth testing of pressure vessel steel in H2 gas supported design-life calculation prescribed in ASME code

## Slide 14: Back-up Slides

## Slide 15: Measurement of da/dN vs. frequency indicates that crack growth rates at 10 Hz are not upper bounds
General trend: da/dN increases as frequency decreases, then reaches plateau value
  Most pronounced for 34CrMo4 steel in 45 MPa H2 gas at DK = 24 MPa m1/2
da/dN vs. f data reveal effects of material and environmental variables
  Higher-strength 34CrMo4 steel generally more susceptible to hydrogen-accelerated fatigue crack growth than lower-strength SA-372 Gr. J steel
  Crack growth rates for SA-372 Gr. J steel equal at 45 and 100 MPa H2 pressure

## Slide 16: Extrapolated and multi-step FCG relationships formulated from multiple data sets
Extrapolated FCG relationship: SA-372 Gr. J at 100 MPa H2 and 0.1 Hz
  Crack growth rates do not vary with H2 pressure above 45 MPa
Multi-step FCG relationship: SA-372 Gr. J at 45 MPa H2 and 4130X in air
  At intermediate and high DK, curve fit to upper-bound crack growth rates
Assumption: relative differences between extrapolated and multi-step FCG relationships maintained at higher R ratios (i.e., R = 0.5 and 0.7)
Air
R=0.7
AISI 4130X
45 MPa H2
R=0.1
SA-372 Gr. J
100 MPa H2
R=0.2
SA-372 Gr. J
multi-step FCG relationship
extrapolated FCG relationship

## Slide 17: Fatigue-life analysis for manufactured vessel: consider extrapolated and multi-step FCG relationships
Double-neck cylinder designed according to EN-1964-1 + 2010/35/EU (TPED qualification)
  220 x 9.1 mm (OD x WT min)
  MAWP = 28 MPa
  Fabricated from 34CrMo4 steel (Sy min = 600 MPa, 780 < Su < 890 MPa): not ASME-qualified, but cylinder thickness compliant with Section VIII-2
  For fatigue-life calculations, assume SA-372 Gr. J steel
extrapolated
multi-step

## Slide 18: Fatigue-life analysis follows fracture mechanics approach using K solutions from API579-1/ASME FFS1
Applied K solution for internally pressurized cylinder with longitudinal-oriented, semi-elliptical surface crack
Crack depth (a) vs. number of cycles (N) calculated from two different fatigue crack growth relationships:
Semi-elliptical defect size and shape:
  Depth: a = 0.455 mm (5% min WT)
  Length: c = 1.365 mm (a/2c = 1/3, as specified in KD-4)
Extrapolated: single power-law relationship fit only to high-DK data
Multi-step: multiple power-law relationships fit to data in low-, intermediate-, and high-DK ranges

## Slide 19: Fatigue crack growth relationship has prominent effect on calculated pressure vessel design life
Developing test procedures that allow construction of reliable multi-step FCG relationship has significant impact
Dp | FCG relationship | Allowable # cycles
14 – 28 MPa (50% MAWP) | extrapolated | 36,000
 | multi-step | 179,000
19.6 – 28 MPa (30% MAWP) | extrapolated | 194,000
 | multi-step | ∞